SECTION 07565                      
    PREPARATION FOR REROOFING

03/11

UTHealth FPE Standard Specification
SECTION 07 32 13
CLAY ROOF TILES
This Standard Specification Section is controlled by the Office of Facilities Planning and Construction, The University of Texas System.  It is to be used as guideline on all UT System projects, unless deviations are approved in writing by the Project Manager.  It is not to be used for bidding, permitting, construction or any other purpose.  This document is the property of UT System, and use of this document, in part or in whole, for any purpose other than for a UT System project may not be done without written permission of UT System.

To receive current updates of standard specification sections, please go to the web site at: www.utsystem.edu/fpc or contact the Office of Facilities Planning and Construction. 

The issuance and revision history of this section is tabulated below.  Unless contractually required for another UT System project, please destroy any previous copy in your possession.

	Rev No.
	Date
	Pages
	Remarks

	0
	January 2007
	11 
	Issuance 

	1
	March 2011
	1
	1.06 B

	
	
	
	

	
	
	
	


UTHealth FPE Standard Specification
SECTION 07 32 13
CLAY ROOF TILES
Hidden Text - Specifier Note: There are numerous types and styles of clay roof tiles.  Specifier to verify specific project requirements related to aesthetics, wind uplift, insulation, color blend and other properties.  This Section includes requirement for a tile color blend mockup.  Clay roof tiles are typically installed over vented attic space.  Consult with clay tile roof manufacture to determine fastening and other requirements over roof board insulation, or compact assemblies
PART 1   GENERAL

1.01 SECTION INCLUDES Verify scope.
A. Clay roof tiles
B. Clay roof tile underlayment and accessories
1.02 RELATED WORK Verify related Sections titles and names.
A. Section 06 10 00 - Rough Carpentry

B. Section 07 62 00 - Sheet Metal Flashing and Trim  Copper, stainless steel or other long-lasting type flashing material is typically specified for use with clay roof tiles.  Coordinate with sheet metal flashing Section.
1.03 REFERENCES Verify appropriate reference standards  
A. National Roofing Contractors Association (NRCA) Roofing and Waterproofing Manual
B. Tile Roofing Institute - Concrete and Clay Roof Tile Installation Manual for Moderate Climate Regions

C. Underwriters Laboratories (UL) 

1. Roofing Materials and Systems Directory

2. Fire Resistance Directory
D. ASTM C270 - Specification for Mortar for Unit Masonry
E. ASTM C1167 - Clay Roof Tiles

F. ASTM D1970 - Self-Adhering Polymer Modified Bituminous Sheet Materials Used as Steep Roofing Underlayment for Ice Dam Protection Verify use – this product might be required in areas of slight slope, or other special areas.  Consult with clay roof tile manufacture to determine acceptable products and use(s).  Delete this reference if not applicable.  Part 2 & 3 of this Section includes product listing for self-adhering underlayment.  Revise these paragraphs to indicate actual Project requirements.
G. ASTM D4586 - Standard Specification for Asphalt Roof Cement, Asbestos Free 
Delete underlayment references below that do not apply. Part 2 of this Section lists one layer ASTM D 6164, Type I, Grade G for standard underlayment.  Revise Part 2 if ASTM D2626, D4869, D6757, or D1970 (see above), or other type of underlayment is utilized
H. ASTM D 2626 - Specification for Asphalt-Saturated and Coated Organic Felt Base Sheet Used in Roofing
I. ASTM D4869 - Standard Specification for Asphalt-Saturated Organic Felt Shingle Underlayment Used in Roofing

J. ASTM D6164 - Specification for Styrene Butadiene Styrene (SBS) Modified Bituminous Sheet Materials Using Polyester Reinforcements
K. ASTM D6757 – Standard Specification for Inorganic Underlayment for Use with Steep Slope Roofing Products
1.04 SUBMITTALS 
A. Submit under provisions of SPECIAL CONDITIONS requirements and Division 1 Section 01 21 00 Submittal Procedures. Verify Division 1 Section number reference and submittal requirements. 
B. Prior to pre-roofing meeting, submit the following:

1. Manufacturer's Certification:  Letter from manufacturer, on letterhead, and signed by authorized representative, stating:

a) Clay roof tile comply with ASTM C1167 Grade 1 and that materials furnished are compatible. Verify ASTM clay tile reference standard.
b) Clay roof tile, fasteners and accessories attached according to this Section meet Project-specific wind resistance requirements. Verify special wind zone requirements, such as coastal.  Certain wind zones may require additional fasteners, hold-down clips, or special adhesive.
c) Clay roof tile, tile accessories and underlayment over roof deck qualifies for specified warranty. 
d) Installer is authorized to install manufacturer's warranty roof systems minimum five (5) years prior to the Project NTP.

2. Sample manufacturer, and installer, warranties meeting Specification requirements.

3. Product Literature:  Submit product literature on roof system and accessory components. 

4. Approved tile blend color selection criteria.  Coordinate with construction of Mockup a subsequent approval of A/E and Owner.

5. Shop drawings.

C. Roof Protection Plan:  Submit written roof protection plan for A/E and Owner approval that describes type and layout of roof protection during construction activities on or above roof area.  Certain projects may require a more detailed approach to roof protection, including consideration of a temporary roof to allow construction to proceed without damaging final roof.
D. Pre-Roofing Meeting Notes:  Submit Pre-Roofing Meeting Notes within 5 business days of meeting date.
E. Manufacturer's Field Reports:  Submit copies of manufacturer's field reports to A/E during the Work, and at final completion.

F. Shop drawings: Submit shop drawings for approval prior to Pre-roofing Conference and start of Work.  Include the following Drawings: Certain projects may require a detailed Shop Drawing submittal.  Below requirements illustrate a comprehensive approach to Shop Drawings. 
1. Roof Plan(s):  Prepare scaled roof plan locating roof details and penetrations.  
2. Location and type of penetrations. Illustrate edge, wall, vent curb and penetrations flashing.  Scale details at 1½” or larger.  Manufacturer’s standard pre-printed details are not acceptable for shop drawings
3. Indicate deck type on each drawing.
4. Indicate location of proposed staging areas and material storage on site plan.
5. Roof Plan indicating clay roof tile fastening types and zones.  Depict attachment types(s) and areas on roof plan for each attachment type.
G. Product data:

1. Submit manufacturer’s data sheets for each product being installed.  Include manufacturer’s installation instructions.

2. Material Safety Data Sheets:  Provide manufacturer’s MSDS information for all materials proposed for use.

3. ASTM Compliance Sheet:  Submit product material list with corresponding ASTM standard(s) each product complies with.  Include Specification paragraph reference number that relates to each product. 
4. Tile samples exhibiting available tile colors.  Coordinate with Mockup construction.  
Clay roof tiles are typically installed over a ¾ inch thick plywood deck over a vented attic with fiberglass batt insulation on floor of attic.  Clay roof tile placed over roof insulation board or a compact roof system (no vented attic) require special design techniques.  Consult with clay roof tile manufacturer for recommendations. Delete below paragraph if convention vented attic is utilized.
5. Board Insulation products:  Submit manufacturer’s data sheets for each component required including insulation board, fasteners and accessories.  Provide roofing system manufacturer’s written acceptance of proposed, insulation, fasteners, and procedures for installation.  Coordinate with 07 22 16.
H. Clay Tile Roof System Mockup:  Construct tile blend mockup and have blend approved prior to ordering tile.  Construct tile mockup to allow adequate lead time in ordering roof tile.
1. Construct 10 foot by 10 foot, ¾ inch thick plywood deck, at ground level, sloped to match predominate Project roof deck slope.  Install nailer at mockup ridge.  Adequately support and anchor Mockup structure to prevent collapse and wind damage.

2. Install complete clay tile roof system components above Mockup roof deck.  

3. Install 4 foot long samples of eave flashings, gutter, closures, ridge tile, pigmented mortar, wind clips and tile fasteners to demonstrate installation and materials.

4. Provide 6 different field tile colors blend chosen by A/E from clay roof tile manufacturer’s color selections.  Coordinate installation of mockup tiles with A/E and Owner’s Representative. Consult Owner’s Representative for tile blend review and approval preferences.  Include language here to define sample colors
5. Obtain tile color blend approval of A/E and Owner prior to ordering clay roof tiles.  Consult Owner’s Representative for final tile approval procedure.  Owner may wish to have a field sample of tile blend installed before final approval of blend is given.  Requirement to install field sample on Project roof deck may affect Project schedule to lead time for tile shipment.
1.05 QUALIFICATIONS

A. Installer:  Company specializing in performing the work of this Section and approved by roof manufacturer for installation of specified roof system.

B. Minimum 5 years documented successful experience with clay tile roofing.

1.06 REGULATORY REQUIREMENTS

A. Fire Resistance: 
1. UL Class A Fire Hazard Classification.  Clay roof tile is one of the products typically exempt from fire testing due to its fire-resistant properties.  
2. UL _______ Roof Ceiling Assembly Rating.  Verify if rated roof ceiling assembly is required 1 hour, 2 hour, etc.  Delete this paragraph if not applicable
B. Wind Uplift Resistance:  design and certify that clay roof tiles meet wind uplift loads as shown on Structural Drawings.   Verify special attachment of clay roof tiles in coastal and other high risk areas.  Roof slope can affect attachment method.  Ensure roof slope(s) are evaluated for tile attachment design.  Consult OFPC Manager for information. 
1.07 TOLERANCES

A. Comply with tolerances listed in this Section.

B. Where tolerances are not expressly stated in these Specifications, or by the manufacturer, perform Work within tolerances specified in the NRCA Roofing and Waterproofing Manual.

1.08 PRE-ROOFING CONFERENCE
A. Schedule meeting to discuss roof Work before start of work onsite.  Notify attending parties prior to commencing work of this Section.  
B. Pre-roofing conference attendees shall include Owner, A/E, A/E’s roofing consultant, General Contractor representatives, roofing subcontractor project manager and superintendent/foreman, related subcontractors and roof manufacturer’s technical representative.
C. Review Specifications, Submittals, installation procedures and coordination required with related Work.  Agenda shall include:
1. Schedule of daily roofing operations and daily production anticipated.
2. Designation of key personnel and their respective responsibilities.

3. Review of staging and material storage locations.

4. Coordination of work with other trades.

5. Emergency rain protection procedures.
6. Protection of completed roofing and Roof Protection Plan.
7. Manufacturer’s scheduled inspections and acceptance procedures.

8. Warranty period process for leak repairs and inspections.
D. Keep meeting notes and provide copies to those in attendance according to Submittal requirements.

1.09 DELIVERY, STORAGE, AND HANDLING

A. Deliver, store, and handle products according to manufacturer's recommendations.

B. Deliver products in original containers, dry, undamaged, with seals and labels intact.

C. Storage: Verify particular jobsite conditions as related to material storage.
1. Roof-top storage of weather-sensitive material is not permitted.  Material stored overnight on roof-top will be considered defective.

2. Note – Select ONE of the following statements:-If site conditions allow storage trailers onsite use the following. 
Store weather-sensitive products in enclosed storage trailers. 
Or if site conditions do not allow storage trailers 
Store weather-sensitive products on pallets, clear of ground, and cover with secure breathable canvas tarps. 
 Or if site conditions do not allow site storage 
Store weather-sensitive products in an enclosed warehouse, or in storage trailers off-site.  Deliver products in quantity that can be used each day, without roof-top storage.  Products must be returned to warehouse, or storage trailer, each day.
3. Store rolls goods on end.  Do not use rolls with damaged ends.  Cut and remove portion of roll damaged, and use undamaged portion.

D. Store related materials, within temperature ranges, recommended by the manufacturer(s) of each product.

1.010 ENVIRONMENTAL REQUIREMENTS

A. Comply with manufacturer’s environmental requirements for storage and application of products.

B. Verify existing and forecasted weather conditions and determine when conditions are acceptable for roof Work within the guidelines as follows:

1. Do not proceed with work when ambient air temperature falls below 40 ˚ F.

2. Do not proceed with roof application when excessive moisture is present.

C. Do not expose materials sensitive to water, or sunlight, damage in quantities greater than can be weatherproofed during each day.

1.011 COORDINATION

A. Coordinate Work with installation of associated metal flashings as the Work of this Section proceeds.

1.012 INSPECTION BY MANUFACTURER Verify Owner preferences.
A. Coordinate inspection of the Work, by an authorized technical representative of the clay roof tile manufacturer.

1. Manufacturer is required to inspect work a minimum of three (3) visits per Project.

2. Manufacturer’s visits to consist of: 

a) Attendance to Pre-Roofing Meeting.

b) One visit at Project commencement.

c) Interim visits for each 10 work days of roof work, and one visit at Project completion.

B. Provide manufacturer's field inspection reports within five days of each site visit.

1.013 MANUFACTURER WARRANTY Verify Owner preferences for roof warranties.  Tiles chosen for a specific appearance or other attribute may affect warranty terms listed below.  If specific tile type is required verify warranty options.
A. Provide manufacturer's fifty (50) year clay roof tile material warranty.  Warranty shall include manufacturer providing replacement tiles for defective materials, including shipping and delivery costs. 
B. Warranty shall be issued on the manufacturer's form as submitted by Contractor and reviewed by A/E.

C. If special maintenance of the roof is required by the manufacturer during the Warranty term(s), such requirements shall be provided to the Owner with the Warranty.

1.014 INSTALLER WARRANTY

A. Roof Installer Warranty:  provide two (2) year installer warranty under provisions of Section 01 70 50 – Project Closeout. Verify Section number.
B. Provide on Midwest Roofing Contractors Association Form 2002B - Roofing Contractor Workmanship Warranty.  Warranty shall be issued on form submitted, and reviewed, prior to Work commencement.  
C. Installer Warranty to be co-signed by General Contractor.

PART 2   PRODUCTS Verify Owner preferences and Project requirements for roof assembly.
2.01 GENERAL

A. Roof System:  ¾ inch thick plywood roof deck, board insulation as specified in Section 07 22 16, one shingled ply of underlayment and clay roof tiles.  Verify roof system components. Delete references to board insulation if not part of roof system.
B. Obtain written approval from clay roof tile manufacturer for use of products incorporated into roof system, which are not supplied by clay roof tile manufacturer.

C. Substitutions:  
1. Where specific products are listed in this Specification, the referenced roofing manufacturer’s systems are to establish a level of quality.  
2. Requests for substitutions to listed products shall be submitted during the bidding phase per requirements of Section 01 21 00.  Verify Section number.
3. Consideration of requests for substitution is at the sole discretion of the A/E and Owner, and approvals shall be issued in writing by the A/E with Owner concurrence.
2.02 MATERIALS
A. Field Tile:  ASTM C1167, Grade 1, Spanish Tile, color blend chosen by A/E. Verify Owner preferences for clay roof tile properties.  Tiles chosen for a specific appearance or other attribute may affect Project schedule.  If specific tile type is required verify warranty options Consider including a list of particular clay roof tile manufacturers, along with specific product name.
B. Tile Closures:  eave and headwall closures, clay tile matching color of field tile, as supplied by clay roof tile manufacture.

C. Ridge and Hip Tiles:  match color of field tiles, as supplied by clay roof tile manufacture.  Provide clay roof tile manufacture-produced ridge and hip terminations and transitions.
D. Tile Nails: Copper or stainless-steel, ring-shank roofing nails, minimum 3/8 inch head, of sufficient length to penetrate 1 inch into, or 1/4 inch through roof deck.  

E. Tile Wind Clips:  brass or stainless steel, as supplied by, or recommended by clay roof tile manufacturer for use with specified tile profile.

F. Underlayment:  ASTM D1970, modified bituminous waterproofing sheet, self-adhering, high temperature resistant, Vycor Ultra by W.R. Grace, or approved substitute. Verify underlayment necessary for Project requirements.  Revise this underlayment reference if  other type of underlayment is utilized
G. Mortar:  ASTM C270, Type M, color pigmented as approved by A/E. 

H. Plastic Cement:  ASTM D4586, non-asbestos reinforced, as supplied and recommended by clay roof tile manufacturer.

I. Sheet metal flashings:  according to provisions of Section 07 62 00. Verify Section number.  Typically flashings for clay tile roofs are long-lasting copper, non-magnetic stainless steel, or similar type metals.
Delete below paragraph if convention vented attic is utilized Board insulation requires special coordination with tile fastening method.  Consult with tile manufacturer before specifying board insulation above roof deck.
J. Board Insulation:  Comply with requirements of Section 07 22 16. Verify Section number.
PART 3 – EXECUTION

3.01 GENERAL

A. Work of this Section shall be performed in accordance with quality workmanship standards as defined by NRCA.  Detailing shall be performed in accordance with standards as defined by NRCA and SMACNA.  

B. Clay roof tile manufacturer’s technical specifications shall be considered a part of this specification and shall be used as a minimum standard in conjunction with this specification.  If this Specification conflicts with, or exceeds manufacturer’s minimum requirements the more rigid standard shall apply and be enforced.

3.02 COORDINATION

A. Ensure proper sequencing of roofing and to allow installation of roof and flashings as detailed, without damage.

B. Coordinate activities to prevent damage to roof assemblies.

3.03 EXAMINATION & PREPARATION
A. Do not store, stage activities, or allow construction traffic over roof areas, unless protection plan is approved in advance by A/E.  

B. Contractor is responsible for maintaining roof in good condition, and shall restore to manufacturer’s warrantable state upon completion of activities.

C. Verify that surfaces and site conditions are ready to receive Work.  Verify that debris has been completely removed from roof area and broom clean the deck immediately prior to roofing application.
D. Verify deck is sound, smooth, and dry enough for covering with roofing.  Report decking not serviceable for covering with roof system.

E. Verify roof openings, curbs, pipes, sleeves, ducts, and vents through roof are solidly set, and wood components are in place.

F. Construct and install decking, nailers and blocking under provisions of Section 06 10 00. Verify Section number.
G. Install sheet metal components, according to provisions of Section 07 62 00. Verify Section number.
3.04 TEMPORARY WATERPROOFING

A. Provide water stops and temporary tie-ins daily to prevent moisture penetration into building interior or installed assemblies. 

B. Seal roofing temporarily to the deck where leakage could penetrate installed assemblies.  Remove upon resumption of Work.

C. Provide permanent, or temporary, counter flashing daily.

D. Provide temporary seals which do not soil finished work surfaces or contaminate surfaces intended to receive sealants.

E. Remove temporary seals from completed Work.

3.05 EXAMINATION OF SITE

A. Inspect and verify pre-existing conditions and appearance of building surfaces, components and grounds.  Submit findings prior to starting Work.

B. Verify deck is clean, dry, smooth and ready to receive roofing.

C. Verify sheet metal flashings are complete and installed in accordance with Sheet Metal Flashings Section 07 62 00. Verify Section number.
Clay roof tiles are typically installed over a plywood deck over a vented attic with fiberglass batt insulation on floor of attic.  Clay roof tiles placed over roof insulation board or a compact roof system (no vented attic) require special design techniques.  Consult with clay roof tile manufacturer for recommendations. Delete below paragraph if convention vented attic is utilized.
3.06 BOARD INSULATION APPLICATION

A. Comply with requirements of Section 07 22 16.  Verify Section number.
B. Only install insulation that can be covered with watertight underlayment the same day. 

C. Protect installed insulation from damage, and moisture.
3.07 UNDERLAYMENT INSTALLATION

A. Comply with tile manufacturer's application instructions.

B. Install one ply, shingle fashion, with minimum 4 inch laps.

C. Install strip-in ply at ridges, hips, valleys, transitions, eaves and rise walls.  

D. Lap shingle-fashion with field underlayment.
E. Do not allow excessive exposure before covering with clay roof tiles.  Comply with manufacturer’s exposure limits.  Remove and replace underlayment that is over-exposed.
3.08 TILE INSTALLATION

A. Apply in accordance with tile manufacturer's recommendations.

B. Match approved Mockup blend pattern and layout.

C. Ensure tile courses are straight and uniform distribution.  Use string lines to ensure straight courses.

D. Fasten each tile to roof deck with 2 fasteners per tile.  Drive fasteners flush without damaging tile.  Verify number of fasteners per tile to meet wind zone requirements.
E. Install tile wind clips at first course of roof tile at eave. Verify special attachment of clay roof tiles in coastal, or high-rise and other high risk areas.  Roof slope can affect attachment method.  Ensure roof slope(s) are evaluated for tile attachment design.  Consult OFPC Manager for information
F. Replace broken tiles.  Remove tile in its entirety, seal nail holes in underlayment with sealant or plastic cement.  Install replacement tile.
G. Install flashings to provide watertight construction.
3.09 HIP & RIDGE TILE INSTALLATION

A. Cover wood nailer with self-adhering strip-in ply.  Lap over underlayment minimum 6 inches.  Ensure shingle-fashion application.

B. Install field tile and apply mortar to head of wetted field tile.

C. Moisten ridge tile and set in mortar bed.  Ensure positive embedment.

D. Fasten hip tile to nailer.  Apply plastic cement at overlap with adjacent hip tile.

3.010 CLEANING & PROTECTION

A. Clean roof surfaces, metal flashings, walls, windows, walks, and other surfaces, which become soiled or discolored due to the work of this Section.

B. Utilize cleaning agents which are approved by the applicable manufacturer.

C. Protect completed Work during construction activities.

D. Remove debris, trash, and extra materials from grounds and roof areas daily.

E. Comply with submitted Roof Protection Plan.: Certain projects may require a more detailed approach to roof protection, including consideration of a temporary roof to allow construction to proceed without damaging final roof
F. Protect roof system from damage.  Repair or remove and replace damaged clay roof tiles according to methods approved by roof manufacturer and A/E.  A/E and Owner’s decision on corrective procedure will be final.
END OF SECTION
AUSTECH ROOF CONSULTANTS INC.

COPYRIGHT 1990                                            07565-12
	Clay Roof Tiles

07 32 13 - Page 1 of 13

	



